## An analytic solution to the SELE of a GaAs wafer

We would like to calculate the SELE of a GaAs wafer.

Assumptions:

- Uniform doped wafer, much thicker than the absorption depth at the wavelength of the PL signal considered and the diffusion length.

- No electric fields

- Step function like photon transmission from the wafer to the ambient: Tf=Tθ<θc and 0 otherwise

- No photon recycling.

### Calculation procedure:

- Calculate the excess electron concentration Δnδ in response to an excitation δx-x0G0

- Calculate the total radiative recombination RradE,x,x0=B'E⋅nx,x0⋅p-n0p0≈B'Ep0Δnδx,x0.

- Photon generation at a specific wavelength is

B'E=4π4π3ℏ3c02ni2αbEnE2E21expE-(EFC(z)-EFV(z))kBT-1≈1π2ℏ3c02ni2αbEnE2E2exp-E-(EFC(z)-EFV(z))kBT

RradE,x,x0=B'p0Δnx,x0≈p0Δnx,x0αbEnE2E2exp-EkBTπ2ℏ3c02ni2

- Calculate the depth dependent escape probability Px

- Calculate the total PL flux: ΦE,x0=0∞RradE,x,x0Pxdx

### The excess electron concentration Δn:

The differential equation:

|  | d2Δndx2=G0Dδx-x0-ΔnLn2 | (1) |
| --- | --- | --- |

Where Ln=τD, and τ=p0B+1τn-1 is the effective lifetime. Notice that G0 has units of 1cm2s⋅eV

Boundary condition at x=0:

|  | DdΔndx=Sn-n0 | (2) |
| --- | --- | --- |

At x0 the electron concentration is continuous, and the current difference is determined by the delta function generation:

|  | Jnx0+-Jnx0-=qG0 | (3) |
| --- | --- | --- |

The solution is in the form of:

|  | Δn=ae-xLn+bexLnx<x0ce-xLnx>x0 | (4) |
| --- | --- | --- |

From the first boundary condition:

|  | DdΔndx0=DLpb-a=Sa+b→a=bD-SLnD+SLn=bA0 | (5) |
| --- | --- | --- |

At point x0:

|  | ae-x0Ln+bex0Ln=ce-x0Ln→b=e-2x0Lnc-a | (6) |
| --- | --- | --- |

Inserting:

|  | b=e-2x0Lnc-a=e-2x0Lnc-bA0→ce-2x0Ln=b+be-2x0LnA0→c=be2x0Ln+bA0 | (7) |
| --- | --- | --- |

Assuming only diffusion currents and using equation (3):

|  | -DLnae-x0Ln-bex0Ln-ce-x0Ln=G0 | (8) |
| --- | --- | --- |

Rearranging:

|  | bex0Ln+ce-x0Ln-ae-x0Ln=LnG0D | (9) |
| --- | --- | --- |

Inserting again:

|  | bex0Ln+be2x0Ln+bA0e-x0Ln-bA0e-x0Ln=LnG0D | (10) |
| --- | --- | --- |

We obtain:

| b=LnG0Dex0Ln+ex0Ln+A0e-x0Ln-A0e-x0Ln= LnG02De-x0Ln | (11) |
| --- | --- |

| a=A0b= LnG02DA0e-x0Ln | (12) |
| --- | --- |

|  | c=LnG02Dex0Ln+A0e-x0Ln | (13) |
| --- | --- | --- |

|  | Δn=LnG02De-x0LnA0e-xLn+exLnx<x0ex0Ln+A0e-x0Lne-xLnx>x0 | (14) |
| --- | --- | --- |

Hence:

|  | Δn=LnG02DA0e-x+x0Ln+ex-x0Lnx<x0A0e-x+x0Ln+e-x-x0Lnx>x0 | (15) |
| --- | --- | --- |

Testing boundary condition at x=0:

DdΔndx=Sn-n0, D-SLnD+SLn=A0

LnG02DDLn-A0e-x0Ln+e-x0Ln=SLnG02DA0e-x0Ln+e-x0Ln

G02-A0+1=SLnG02DA0+1

D-A0+1=SLnA0+1

D-A0D=A0SLn+SLn

D-SLn=A0SLn+A0D→A0=D-SLnSLn+D

### Depth dependent escape probability:

We assume that the transmission through the surface follows: Tf=Tθ<θc and 0 other wise.

If at the wavelengths considered the wafer thickness is significantly higher than the absorption depth, second order reflections do not have to be considered. Thus:

|  | Pescx=T4π0θc02πe-αxcosθsinθdθdϕ=T20θce-αxcosθsinθdθ | (16) |
| --- | --- | --- |

The solution is:

|  | Pesc'x=T2-cosθe-αxcosθ-αxEi-αxcosθθ=0θ=θc=T2e-αx-cosθce-αxcosθc-αxEi-αxcosθc-Ei-αx | (17) |
| --- | --- | --- |

The function Ei(t) is defined as:

|  | Eit=t∞e-zzdz→Ei-αxcosθ-Ei-αxcos0=-αxcosθc∞e-zzdz--αx∞e-zzdz=-αxcosθc∞e-zzdz+∞-αxe-zzdz=-αxcosθc-αxe-zzdz | (18) |
| --- | --- | --- |

Inserting:

|  | Pesc'x=Te-αx-cosθce-αxcosθc-αx-αxcosθc-αxe-zzdz | (19) |
| --- | --- | --- |

### Photon emission

The PL photon flux now follows:

|  | Φx0,E=0∞Rradx,x0,EPx,Edx | (20) |
| --- | --- | --- |

|  | Φx0,E=0∞0θc02π14πRradx,x0,EPx,E,θdϕdθdx | (21) |
| --- | --- | --- |

|  | Φx0,E=0∞14πRradx,x0,E0θc02πPx,E,θdϕdθdx | (22) |
| --- | --- | --- |

|  | Φx0,E=0∞14πRradx,x0,E2π0θcPx,E,θdθdx | (23) |
| --- | --- | --- |

|  | Φx0,E=0∞12Rradx,x0,E0θcTθe-αxcosθsinθdθdx | (24) |
| --- | --- | --- |

Inserting:

|  | Φx0,E=0∞Rradx,x0,E0θcTθ2e-αxcosθsinθdθdx | (25) |
| --- | --- | --- |

Since all the arguments are strictly positive, We can switch the order of integration (Fubini’s theorm):

|  | Φx0,E=T20θc0∞Rradx,x0,Ee-αxcosθsinθdxdθ | (26) |
| --- | --- | --- |

Thus we obtain:

|  | Φx0,E=T20θc0∞B'p0Δnδx,x0e-αxcosθsinθdxdθ | (27) |
| --- | --- | --- |

Inserting:

|  | Φx0,E=TB'Ep020θcE0∞Δnδx,x0e-αxcosθsinθdxdθ | (28) |
| --- | --- | --- |

Since the escape cone of most semiconductors is very narrow, a first order cosθ≈1, and sinθ≈θwill not result in substantial errors. Thus:

|  | Φx0,E≈TB'Ep020∞Δnδx,x0e-αx0θcsinθdθdx=TB'Ep01-cosθc20∞Δnδx,x0e-αxdx | (29) |
| --- | --- | --- |

Inserting Δnδx,x0:

|  | Φx0,E=TB'Ep02LnG01-cosθc2D0x0A0e-x+x0Ln+ex-x0Lne-αxdx+ex0Ln+A0e-x0Lnx0∞e-xLne-αxdx | (30) |
| --- | --- | --- |

Finally, we obtain:

|  | Φx0,E=TB'Ep02LnG01-cosθc2De-x0Ln0x0A0e-x1Ln+α+ex1Ln-αdx+ex0Ln+A0e-x0Lnx0∞e-x1Ln+αdx | (31) |
| --- | --- | --- |

We not α-=1Ln-α=1-αLnLn, and α+=1Ln+α=1+αLnLn,

TB'Ep0LnG01-cosθc4D=K

|  | Φx0,E=Ke-x0Ln0x0A0e-α+x+eα-xdx+ex0Ln+A0e-x0Lnx0∞e-α+xdx | (32) |
| --- | --- | --- |

Notice that K has units of 1cm3eVs and that the spectrum Φx0,E is written (and integrated) in terms of energy

|  | Φx0,E=Ke-x0Ln-A0e-xα+1Ln+α+ex1Ln-α1Ln-α0x0+ex0Ln+A0e-x0Lne-α+x0α+ | (33) |
| --- | --- | --- |

Rearranging:

|  | Φx0,E=Ke-αx01Ln-α-A0e-x02Ln+α1Ln+α-e-x0Ln1Ln-α+A0e-x0Ln1Ln+α+e-αx0+A0e-x02Ln+α1Ln+α | (34) |
| --- | --- | --- |

We not α-=1Ln-α=1-αLnLn, and α+=1Ln+α=1+αLnLn,

|  | Φx0,E=Ke-αx0α--A0e-x02Ln+αα+-e-x0Lnα-+A0e-x0Lnα++e-αx0+A0e-x02Ln+αα+ | (35) |
| --- | --- | --- |

|  | Φx0,E=Ke-αx0-e-x0Lnα-+A0e-x0Ln+e-αx0α+ | (36) |
| --- | --- | --- |

Φx0,E=K1α-+1α+e-αx0+A0α+-1α-e-x0Ln

1α-+1α+=Ln1-αLn+Ln1+αLn=Ln1+αLn+1-αLn1-αLn2=2Ln1-αLn2

A0α+-1α-=A0Ln1+αLn-Ln1-αLn

The spatially resolved ELE is simply  Spx0,E=Φx0,EG0:

|  | Spx0,E=KG02Ln1-αLn2e-αx0+A0Ln1+αLn-Ln1-αLne-x0Ln | (37) |
| --- | --- | --- |

A0=D-SLnSLn+D

KG0= TB'Ep0Lnθc4D

KG0=TB'Ep0Ln1-cosθc4D

|  | Spx0,E=KLn1-αLn22e-αx0+A0-1-LnαA0+1e-x0Ln | (38) |
| --- | --- | --- |

|  | Spx0,E=TB'Ep0Ln2(1-cosθc4D1-αLn22e-αx0+A0-1-LnαA0+1e-x0Ln | (39) |
| --- | --- | --- |

|  | Spx0,E=TB'Ep0τeff(1-cosθc41-αLn22e-αx0+A0-1-LnαA0+1e-x0Ln | (40) |
| --- | --- | --- |

|  | Spx0,E=K12e-αx0+A0-1-LnαA0+1e-x0Ln | (41) |
| --- | --- | --- |

K1=TB'Ep0τeff1-cosθc41-αLn2

Noting A1=A0-1-LnαA0+1

|  | Spx0,E=K12e-αx0+A1e-x0Ln | (42) |
| --- | --- | --- |

Calculating the incident wavelength dependent PL spectrum for a thick sample:

Assuming a sample illuminated with wavelength λi which corresponds to aborption coefficient αi.

The optical generation normalized by the absorbed photon flux is:

|  | G(λi,x)=αie-αix | (43) |
| --- | --- | --- |

### The incident wavelength dependent PL spectrum

Thus, the PL spectrum resulting from this illumination is:

|  | ΦPLλi,E=0∞Gλi,xSpE,xdx | (44) |
| --- | --- | --- |

Inserting:

|  | ΦPLλi,E=αiK10∞e-αix2e-αx+A1e-xLndx | (45) |
| --- | --- | --- |

|  | ΦPLλi,E=αiK10∞2e-α+ αix+A1e-1Ln+αixdx | (46) |
| --- | --- | --- |

|  | ΦPLλi,E=-αiK12e-α+ αixα+ αi+A1e-1Ln+αix1Ln+αi0∞=αiK12α+ αi+A11Ln+αi | (47) |
| --- | --- | --- |

K1=TB'Ep0τeff(1-cosθc41-αLn2

A1=A0-1-LnαA0+1

### Relating Sp to S

The SELE is the weighted average spatially resolved SELE:

|  | Sx=0∞Spx,EdE | (48) |
| --- | --- | --- |

The analytic solution underestimates the SELE when photon recycling is probable. This results to lower values at low SRV near the surface (high ILE and high escape probability) and when the bulk lifetime is high (high ILE). The figures below were calculated with the bandgap “artificially at 1.4 (which assumes some band gap narrowing), and at a temperature of 299K. All other parameters are as in the paper.

### Obtaining results by fitting to the ratio of two spectra

As discussed above:

|  | ΦPLλi,E=αiK12α+ αi+A11Ln+αi=K12αiα+ αi+A1αiLn1+αiLn==K12αi(1+αiLn)(α+ αi)(1+αiLn)+A1αiLnα+ αi(α+ αi)(1+αiLn)==K12αi1+αiLn+A1αiLnα+ αi(α+ αi)(1+αiLn) | (49) |
| --- | --- | --- |

K1=TB'Ep0τeff(1-cosθc41-αLn2

A1=A0-1-LnαA0+1

A0=D-SLnSLn+D=Dτ -SDτ+S

Thus, the ratio between two PL spectra measured with two incident wavelengths follows:

|  | R=ΦPLλi,EΦPLλi,ref,E=2αi1+αiLn+A1αiLnα+ αi(α+ αi)(1+αiLn)2αi,ref1+αi,refLn+A1αi,refLnα+ αi,ref(α+ αi,ref)(1+αi,refLn)=2αi1+αiLn+A1αiLnα+ αi α+ αi,ref1+αi,refLnα+ αi1+αiLn 2αi,ref1+αi,refLn+A1αi,refLnα+ αi,ref | (50) |
| --- | --- | --- |

Assuming that the absorption coefficients for the incident illumination are known, the fitted parameters in equation (50) are the diffusion length, A0 which is determined by the surface recombination, and the absorption coefficient for the PL photons (those are hard to measure).

If the absorption coefficient for the incident and reference beams are much larger than for the PL emitted photons (which is reasonable), α+ αi≈αi  and α+ αi,ref≈αi,ref, equation (50) becomes:

|  | RE=2αi1+αiLn+A1αi2Ln αi,ref1+αi,refLnαi1+αiLn 2αi,ref1+αi,refLn+A1αi,ref2Ln==21+αiLn+A1αiLn αi,ref1+αi,refLn1+αiLn 2αi,ref1+αi,refLn+A1αi,ref2Ln==1+αi,refLn21+αiLn+A1αiLn 1+αiLn 21+αi,refLn+A1αi,refLn | (51) |
| --- | --- | --- |

For one value of E we have A1E, Ln. Thus, repeating the process for another incident wavelength, A1E, and Ln can be found. Hence, a minimum of 3 incident wavelengths are required.

This allows calculating eventually, Ln, A0, and αE

The fitting process should be as follows:

- Fit the ratio (which is insensitive to the alpha) to obtain Ln and S.

- Fix Ln and S and find a fit to the alpha by fitting the spectra.

This can be done in an iterative process…

Hwang J App Phys 1969 conducted a PL based analysis in which he used the absorption coefficients near the band gap as inputs to obtain the surface recombination velocity and diffusion length. Our analysis is very similar to his. By looking at the PL induced at different wavelengths we can remove the need to measure the absorption coefficient at wavelengths near the band edge (which is difficult).

Things to think about:

- Expand analysis to films with surface recombination at the back surface.

  - Add a second term for PL photons reflected off the back surface?

  - The absorption should remain exponential

  - For thin films and defects PL- can we assume that no PL photons are absorbed?

  - It is probably more interesting to look at the spectral SELE of sub bandgap emission than to apply the analytical method to simple wafers (as in Hwang). The analytical method should be OK here.

  - Is it possible that the discrepancy with Tamir’s simulation is related to improper use of alphas and FCA?